Table 1 Salmon calcitonin solutions composition intended for spray drying. t.s.c.–total solute concentration

| Sugar | Peptide:sugar ratio (w/w) | t.s.c. (%) | Abbreviation |
| --- | --- | --- | --- |
| d-(+)-raffinose pentahydrate | 5:95 | 2.9 | sCT:R |
| d-(+)-raffinose pentahydrate:hydroxypropyl-β-cyclodextrin | 5:57:38 | 2.9 | sCT:R:HPβCD |
|  | 5:38:57 |  |  |
| d-(+)-trehalose dihydrate | 5:95 | 1 | sCT:T |
| d-(+)-trehalose dihydrate:hydroxypropyl-β-cyclodextrin | 5:67:28 | 1 | sCT:T:HPβCD |
|  | 5:57:38 |  |  |
|  | 5:38:57 |  |  |
|  | 5:28:67 |  |  |

Table 2 Particle size, specific surface area (SSA), true density (true den.), bulk density (bρ), tap density (tρ), calculated aerodynamic diameter (daer), glass transition temperature (Tg) and residual solvent content (RSC) by TGA and GC-FID of sCT: sugar composite systems.

|  |  | sCT:R 5:95 | sCT:R:HPβCD 5:57:38 | sCT:R:HPβCD 5:38:57 | sCT:T 5:95 | sCT:T:HPβCD 5:67:28 | sCT:T:HPβCD 5:57:38 | sCT:T:HPβCD 5:38:57 | sCT:T:HPβCD 5:28:67 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| d50 (µm) |  | 1.8±0.05 | 1.7±0.01 | 1.9±0.04 | 1.8±0.01 | 1.5±0.02 | 1.6±0.00 | 1.6±0.00 | 1.6±0.00 |
| SSA (m2/g) |  | 55.34±0.15 | 99.45±0.74 | 102.84±0.06 | 58.47±0.04 | 91.37±1.17 | 104.1±1.85 | 103.53±1.88 | 98.87±9.48 |
| bρ(g/cm3) |  | 0.22±0.00 | 0.19±0.01 | 0.20±0.00 | 0.17±0.00 | 0.20±0.01 | 0.18±0.01 | 0.16±0.01 | 0.23±0.00 |
| tρ (g/cm3) |  | 0.37±0.01 | 0.34±0.01 | 0.33±0.01 | 0.29±0.00 | 0.34±0.01 | 0.33±0.02 | 0.29±0.01 | 0.39±0.01 |
| daer (µm) |  | 2.2±0.02 | 1.4±0.00 | 1.6±0.00 | 2.2±0.01 | 1.9±0.00 | 1.9±0.01 | 1.9±0.00 | 1.8±0.01 |
| Tg (°C) |  | 114.7±0.77 | 144.5±0.44 | 159.2±0.43 | 120.3±1.43 | 139.7±1.49 | 142.5±0.15 | 153.0±0.40 | 182.7±2.76 |
| RSC by TGA (% w/w) |  | 2.7±0.45 | 3.3±0.33 | 3.5±0.6 | 3.4±0.6 | 3.6±0.5 | 5.0±0.4 | 4.2±0.9 | 4.9±0.1 |
| RSC by GC-FID (% w/w) | MeOH | ND | 0.09±0.00 | 0.16±0.02 | 0.52±0.00 | 0.73±0.01 | 0.80±0.02 | 0.99±0.01 | 0.88±0.01 |
|  | BA | 0.48±0.03 | 1.50±0.01 | 1.72±0.05 | 0.58±0.08 | 1.93±0.01 | 1.55±0.01 | 1.82±0.06 | 1.53±0.04 |
| Extrapolated Water content (%) |  | 2.22 | 1.71 | 1.62 | 2.3 | 0.94 | 2.65 | 1.39 | 2.49 |

Table 3. Salmon calcitonin (sCT) loading in powders by HPLC and Amide I region band area overlap with native sCT of freshly spray-dried sCT:raffinose and sCT:trehalose composite systems and after storage at 25°C/< 5% RH and 4°C/< 5% RH .

|  | Freshly Spray-dried | Storage at 4°C/ 5% RH |  |  | Storage at 25°C/ 5% RH |  |  | sCT loading freshly of spray-dried powders % (w/w) | sCT loading after 24 weeks storage at 4 °C/< 5 % RH (%, w/w) | sCT loading after 24 weeks storage at 25 °C/< 5 % RH (%, w/w) | sCT Bioactivity of spray-dried powders % | sCT Bioactivity after 24 weeks storage |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Week 4 | Week 12 | Week 24 | Week 4 | Week 12 | Week 24 |  |  |  |  | 4 °C/< 5 % RH | 25 °C/< 5 % RH |
| sCT:R | 94 | 84 | 74 | 76 | 84 | 85 | 54 | 5.2±0.03 | 4.4±0.17 | 3.0±0.00 | 102±1.4 | 97.9±19.7 | 106.2±3.1 |
| sCT:R:HPβCD 5:57:38 | 92 | 71 | 71 | 55 | 84 | 56 | 45 | 4.8±0.03 | 3.0±0.03 | 2.40±.03 | 107±5.4 | 81.4±5.3 | 76.8±9.6 |
| sCT:R:HPβCD 5:38:57 | 71 | 54 | 53 | 50 | 54 | 52 | 51 | 3.7±0.01 | 2.8±0.01 | 2.8±0.003 | 112±17.5 | 91.5±7.1 | 70.8±10.8 |
| sCT:T | 70 | 72 | 74 | 61 | 79 | 59 | 50 | 4.3±0.07 | 3.2±0.01 | 2.7±0.01 | 86.5±2.8 | 34.8±7.8 | 31.7±2.2 |
| sCT:T:HPβCD 5:67:28 | 69 | 69 | 65 | 66 | 73 | 67 | 54 | 4.0±0.01 | 3.6±0.03 | 2.9±0.01 | 91.6±34.1 | 24.2±6.6 | 59.1±17.1 |
| sCT:T:HPβCD 5:57:38 | 74 | 68 | 68 | 66 | 73 | 70 | 67 | 4.2±0.01 | 3.6±0.02 | 3.6±0.01 | 71.0±13.7 | 22.8±12.8 | 51.7±13.7 |
| sCT:T:HPβCD 5:38:57 | 87 | 74 | 74 | 56 | 74 | 76 | 57 | 4.8±0.01 | 3.0±0.09 | 3.0±0.08 | 69.8±2.6 | 31.9±2.8 | 41.2±1.2 |
| sCT:T:HPβCD 5:28:67 | 80 | 69 | 58 | 37 | 79 | 76 | 51 | 4.4±0.02 | 2.0±0.011 | 2.7±0.01 | 90.7±28.4 | 58.4±22.4 | 56.8±13.1 |

Table 4 Recovered emitted dose, fine particle fraction (FPF), mass median aerodynamic diameter (MMAD) and geometric standard deviation (GSD) of in vitro aerosol deposition of spray dried composite systems.

|  | sCT:R | sCT:R:HPβCD 5:57:38 | sCT:R:HPβCD 5:38:57 | sCT:T | sCT:T:HPβCD 5:67:28 | sCT:T:HPβCD 5:57:38 | sCT:T:HPβCD 5:38:57 | sCT:T:HPβCD 5:28:67 | sCT:T:HPβCD 5:67:28 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| % recovered emitted dose | 81.1±5.38 | 91.5±1.87 | 91.7±0.77 | 48.5±9.04 | 84.6±1.61 | 87.5±1.88 | 88.5±1.72 | 85.3±4.02 | 84.6±1.61 |
| FPF < 5 µm (%) < 3 µm (%) | 62.8±8.21 50.5±6.84 | 84.5±2.13 81.7±2.19 | 82.1±4.96 74.4±3.99 | 45.5±7.72 35.6±0.99 | 76.3±1.89 69.5±1.54 | 80.7±4.01 76.8±6.91 | 80.5±2.22 75.2±2.52 | 86.8±3.83 83.8±4.99 | 76.3±1.89 69.5±1.54 |
| MMAD (mm) | 2.6±0.05 | 2.1±0.08 | 2.3±0.27 | 4.7±0.21 | 2.3±0.03 | 2.3±0.28 | 2.2±0.08 | 1.9±0.18 | 2.3±0.03 |
| GSD | 2.0±0.09 | 2.0±0.02 | 2.2±0.11 | 2.8±0.19 | 2.1±0.02 | 2.0±0.09 | 2.1±0.04 | 1.94±0.04 | 2.1±0.02 |

Table 5 Phamacokinetic parameters of sCT in rats after intratracheal delivery (mean ± SD, n=5).

|  | sCT solution iv | sCT solution pulm | sCT:R 5:95 | sCT:R:HPbCD 5:57:38 | sCT:T 5:95 |
| --- | --- | --- | --- | --- | --- |
| Dose (µg/kg) | 84±6.95 | 94±12.3 | 146±21.3 | 124±9.9 | 124±16.9 |
| AUC0∞ (µg.h/l) | 180.4±37.36 | 22.4±4.70 | 36.5±13.80 | 39.5±4.29 | 27.8±3.32 |
| Cmax (µg/l) |  | 15.8±5.06 | 33.8±12.97 | 42.5±8.73 | 11.0±4.14 |
| tmax (h) |  | 0.07±0.05 | 0.1±0.06 | 0.1±0.06 | 0.2±0.12 |
| Cl (l/h/kg) | 0.53±0.11 |  |  |  |  |
| Clpulm (l/h/kg) |  | 0.05±0.01 | 0.05±0.01 | 0.03±0.01 | 0.05±0.01 |
| MRT (h) | 0.59±0.06 | 2.0±0.73 | 1.3±0.10 | 1.3±0.18 | 2.2±0.93 |
| MAT (h) |  | 1.2±0.97 | 0.5±0.37 | 0.6±0.45 | 1.2±0.93 |
| t1/2β (h) | 0.6±0.11 | 1.5±0.68 | 0.8±0.07 | 0.9±0.06 | 0.6±0.48 |
| Fabs (%) |  | 11.3±3.01 | 11.5±3.48 | 14.9±2.01 | 10.1±1.37 |
| Frel (%) |  |  | 104±31.5 | 135±18.24 | 74.9±25.91 |