List of Tables

Metformin Hydrochloride and Sitagliptin Phosphate Fixed Dose Combination Product Prepared Using Melt Granulation Continuous Processing Technology

Jeremiah F. Kelleher#1, Atif M. Madi#1, Gareth C. Gilvary2, Y. W. Tian2, Shu. Li2, Ammar Almajaan2, Zoe S. Loys2, David S. Jones2, Gavin P. Andrews2, Anne Marie Healy1*

Affiliation

1School of Pharmacy and Pharmaceutical Sciences, Trinity College Dublin, Dublin, Ireland.

2Pharmaceutical Engineering Group, School of Pharmacy, Queen’s University Belfast, Belfast, Northern Ireland.

# Both authors contributed equally to this work

*Corresponding author:

Prof. Anne Marie Healy

Tel: +35318961444

Email: healyam@tcd.ie

Table I. Specification of Rondol 10 mm Microlab extruder.

| Specification | Value | Unit |
| --- | --- | --- |
| Screw diameter | 10 | mm |
| Screw speed | 0~200 | rpm |
| Profile | Co-rotating, intermeshing | - |
| Number of barrel heating sections | 4 | - |
| Length of each barrel section | 05:01 | L/D |
| Overall barrel length | 20:01 | L/D |
| Minimum run size | 10 | g |
| Typical wastage | <3 | g |
| Maximum processing temperature | 300 | °C |
| Materials of construction of the barrel | High strength carbon steel | - |
| Cooling water requirement | 1 | L/min |

Table II. Summary and composition and processing temperature for optimised formulations.

| Proportion (% w/w) of components in MG formulation |  |  |  |
| --- | --- | --- | --- |
| MET | SIT | PEG 3350 | HPC-A or HPC-S |
| 80 | 6.00 | 4.0 | 10.0 |
| Processing Temperature (°C) |  |  |  |
| Feed Zone | Zone 1 | Zone 2 | Zone 3 |
| 130 | 150 | 170 | 180 |

Table III. Overview of particle size analysis (PSA) results (median particle size, d50) of API raw materials and processed MG formulations.

| Sample | Particle size (d50) (µm) |
| --- | --- |
| MET | 115.08 ± 10.88 |
| SIT | 28.64 ± 0.80 |
| MG HPC-A formulation | 221.67 ± 13.80 |
| MG HPC-S formulation | 281.67 ± 55.05 |

Table IV. Summary of flow parameters of physical mixtures (PM), manufactured melt granules (MG) and manufactured MG materials with glidant.

| Sample | AIF, º | Cohesion, kPa | FF |
| --- | --- | --- | --- |
| PM MET SIT HPC-A PEG | 31.45 ± 1.06 | 0.81 ± 0.13 | 5.61 ± 0.84 |
| PM MET SIT HPC-S PEG | 32.01 ± 2.55 | 0.84 ± 0.18 | 5.57 ± 0.85 |
| MG MET SIT HPC-A PEG | 32.00 ± 1.56 | 1.05 ± 0.13 | 4.74 ± 0.69 |
| MG MET SIT HPC-S PEG | 34.30 ± 1.28 | 0.79 ± 0.18 | 5.38 ± 1.32 |
| MG MET SIT HPC-A PEG and glidant (10 % w/w) | 30.45 ± 1.15 | 0.85 ± 0.09 | 5.41 ± 0.84 |
| MG MET SIT HPC-S PEG and glidant (10 % w/w) | 31.80 ± 1.73 | 0.74 ± 0.14 | 5.21 ± 0.45 |

Table V. Dimensions of melt granulation (MG) manufactured caplets post compression at different compression forces.

| Sample | MG HPC-A formulation |  | MG HPC-S formulation |  |
| --- | --- | --- | --- | --- |
| Compression force to form caplets (N) | 5000 | 8000 | 5000 | 8000 |
| L (mm) | 21.39 ± 0.02 | 21.43 ± 0.03 | 21.41 ± 0.02 | 21.44 ± 0.02 |
| D (mm) | 10.52 ± 0.02 | 10.52 ± 0.02 | 10.52 ± 0.02 | 10.51 ± 0.03 |
| t (mm) | 6.32 ± 0.01 | 6.03 ± 0.05 | 6.14 ± 0.02 | 5.93 ± 0.03 |
| w (mm) | 3.93 ± 0.01 | 3.59 ± 0.08 | 3.58 ± 0.08 | 3.23 ± 0.09 |

Table VI. Results of the tablet hardness test, friability test and disintegration times for MG formulations compressed into caplets at different compression forces.

| Sample | MG HPC-A formulation caplets |  | MG HPC-S formulation caplets |  |
| --- | --- | --- | --- | --- |
| Compression force to form caplets (N) | 5000 | 8000 | 5000 | 8000 |
| Tensile strength of Melt Granulation products (MPa) | 0.22 ± 0.01 | 0.31 ± 0.01 | 0.28 ± 0.03 | 0.44 ± 0.05 |
| Friability of Melt Granulation caplets (%) | 65.53 % (Fail) | 81.08 % (Fail) | 91.96 % (Fail) | 99.25 % (Pass) |
| Disintegration of Melt Granulation caplets (seconds) | 70 ± 12 | 257 ± 55 | 235 ± 35 | 748 ± 28 |