SUPPLEMENTARY MATERIAL

Optimising the in vitro and in vivo performance of oral cocrystal formulations via spray coating

Dolores R. Serranoa,b,c*, David Walsha,b,  Peter O’Connella, Naila A. Mugheirbid, Zelalem Ayenew Workua,b, Francisco Bolas-Fernandezc, Carolina Galianae, Maria Auxiliadora Dea- Ayuelae, Anne Marie Healya,b

aSchool of Pharmacy and Pharmaceutical Sciences, Trinity College Dublin, Dublin 2, Ireland.

bSSPC, Synthesis and Solid State Pharmaceutical Centre, Ireland.

cSchool of Pharmacy, Universidad Complutense de Madrid, Plaza Ramón y Cajal s/n, 28040-Madrid, Spain.

dDepartment of Industrial and Physical Pharmacy, Purdue University, West Lafayette, IN  47907-2091, USA.

eDepartamento de Farmacia, Facultad de Ciencias de la Salud, Universidad CEU Cardenal Herrera, Edificio Seminario s/n, 46113-Moncada, Valencia, Spain

*Corresponding authors:

Dolores R. Serrano

Department of Pharmaceutical Technology

School of Pharmacy

Universidad Complutense de Madrid

Plaza Ramon y Cajal s/n

28040-Madrid, Spain.

Email: drserran@ucm.es

Anne Marie Healy

School of Pharmacy and Pharmaceutical Sciences

Trinity College Dublin

Dublin 2, Ireland.

Tel.: +353 1 896 1444

E-mail address: healyam@tcd.ie

Table S1. Target product profile (TPP) elements for cocrystal-coated inert cores.

| TPP Elements | Target | Justification |
| --- | --- | --- |
| Dosage form (capsules) | Cocrystal-coated on inert cores | Cocrystal engineering can enhance the oral bioavailability of poorly bioavailable drug such as sulfadimidine |
| Route of administration | Oral | Recommended route for delivery of sulfadimidine for the management of antimicrobial infection |
| Dosage type | Fast release | Faster onset of action leading to enhanced oral bioavailability and consequently fast drug dissolution is required |
| Pharmacokinetics | Higher Cmax and AUC | Required for achieving higher drug levels into the blood stream to enhance therapeutic action |
| Packaging | Capsules | Coated inert cores can be easily packed in capsules for improved patient compliance portability and ease of manufacturing due to good powder flowability |
| Stability | At least 24 months at room temperature | To maintain drug efficacy during storage period. Cocrystals ensures higher storage stability than amorphous dispersions. |

Table S2.	Critical quality attributes (CQAs) for cocrystal-coated inert cores containing SDM and rational justification.

| Critical Quality Attributes |  | Target | Is this a CQA? | Rational justification |
| --- | --- | --- | --- | --- |
| Physical attributes | Colour | Acceptable to patients | No | Colour, odour and appearance were not considered as critical, as these are not directly linked to patient efficacy and safety. |
|  | Odour | No unpleasant odour |  |  |
|  | Appearance | Acceptable to patients |  |  |
| Content uniformity (RSD, %) |  | ≤ 1% | Yes | Content uniformity affect drug safety and efficacy, for this reason a homogeneous cocrystal-coating layer was considered as moderately critical. |
| Drug release in 30 min (%) |  | ≥50% | Yes | In vitro dissolution performance of the dosage form, during early dissolution phase is considered critical as will dictate the pharmacokinetic profile and efficacy of the drug. |
| Crystallinity content (%) |  | ≥ 90% | Yes | Percentage of crystallinity is regarded highly critical as determines the solid state and stability of the drug and creation of unintentional co-amorphous should be minimised. |
| Loading efficiency (%) |  | ≥ 20% | Yes | Loading efficiency should be maximised as the amount of SDM administered in patients is moderately high. |

Figure S1. Ishikawa fish-bone diagram depicting various causes and sub-causes affecting the spray coating process.

Table S3. Model generation and predicted equations obtained from the Box-Behnken DoE.

| Model (p-value) | Predicted equation in terms of actual factors |
| --- | --- |
| Two factor interaction (p< 0.01) | Crystallinity= +79.17 -15.24*Atomisation pressure- 0.21*Amount of mass sprayed +2.43*Amount of binder +1.36*Atomisation pressure*Amount of mass sprayed -2.04*Atomisation pressure*Amount of binder -0.06*Amount of mass sprayed*Amount of binder |
| Linear (< 0.0001) | Loading efficiency= -0.36 -2.87*Atomisation pressure +0.53*Amount of mass sprayed +0.08*Amount of binder |
| Two factor interaction (p< 0.12) | Attrition= -39.17 -59.16*Atomisation pressure -0.98*Amount of mass sprayed -0.04*Amount of binder -1.47*Atomisation pressure*Amount of mass sprayed -0.03*Atomisation pressure*Amount of binder +0.003*Amount of mass sprayed*Amount of binder |
| Linear (p<0.03) | Yield= -101.08 -11.28*Atomisation pressure -0.47*Amount of mass sprayed -0.21*Amount of binder |
| Linear (p<0.09) | Log10(RSD)= +0.63 +0.17*Atomisation pressure -0.03*Amount of mass sprayed -0.002*Amount of binder |

Figure 2SA. 3D response surface (a, b, c) and 2D contour plots (e, f, g) showing the influence of the atomization pressure, the amount of sprayed mass and the amount of binder on the yield.

Figure S2B. 3D response surface (a, b, c) and 2D contour plots (e, f, g) showing the influence of the atomization pressure, the amount of sprayed mass and the amount of binder on the percentage of attrition.

Figure S3. 3D response surface (a, b, c) and 2D contour plots (e, f, g) showing the influence of the atomization pressure, the amount of sprayed mass and the amount of binder on content uniformity (RSD).

Table S4. Results of numeric optimization of cocrystal-coated beads.

|  | Constrains (Goals) | Lower limit | Upper limit |
| --- | --- | --- | --- |
| Factors |  |  |  |
| Amount of binder (%) | In range | -1 | +1 |
| Amount of sprayed mass (%) | In range | -1 | +1 |
| Atomisation pressure (Bar) | In range | -1 | +1 |
| Response |  |  |  |
| Loading efficiency (%) | Maximisation | 4.9 | 24.7 |
| Degree of crystallization (%) | Maximisation | 65.9 | 96.0 |
| Yield (%) | In range | 70.5 | 91.9 |
| Attrition (%) | In range | 0.01 | 19.41 |
| RSD (%) | In range | 0.03 | 5.09 |
| Optimised formulation |  |  |  |
| Amount of binder (%) | 5 | - | - |
| Amount of sprayed mass (%) | 45 | - | - |
| Atomisation pressure (Bar) | 0.75 | - | - |

| Response | Experimental Results |  |  |  |  | Predicted results |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Experiment Run 1 | Experiment Run 2 | Experiment Run 3 | Mean | SD | Predicted | Percent Error | 95% CI low | 95% CI high |
| Loading efficiency (%) | 22.51 | 22.11 | 20.50 | 21.71 | 1.06 | 22.07 | 1.06 | 19.54 | 24.61 |
| Degree of crystallinity (%) | 93.48 | 97.47 | 94.49 | 95.15 | 2.07 | 96.21 | 0.76 | 87.99 | 104.41 |

Table S5. Comparison of experimental results with predicted responses. Key: CI, Confidence intervals.

Figure S4. XRD patterns. Key: a- SDM raw material; b- 4ASA raw material; c-Physical mixture of SDM:4ASA (1:1 molar ratio); d- SDM:4ASA polymorph I generated by milling; e- SDM:4ASA polymorph II generated by solvent evaporation; f- SDM:4ASA polymorph II generated by spray drying; g- Blank non-pareil sugar 500 µm beads; h- SDM-4ASA cocrystal polymorph II coated on non-pareil sugar 500 µm beads.

Figure S5. Effect of PVPK90 concentration on cocrystal formation during spray coating. Key: The percentage of the degree of crystallinity and loading efficiency are represented in red and black respectively.

Figure S6. Effect of bead and batch size on cocrystal formation during spray coating. Key: The percentage of the degree of crystallinity and loading efficiency for the 5 g batch size are represented in red and black respectively and for the 25 g batch size in green and blue.

Figure S7. Effect of PVPK90 concentration on water content and surface area during spray coating.

Figure S8. Effect of PVPK90 concentration on the SDM release.

Figure S9. Dissolution profile of SDM:4ASA cocrystal coated beads (in red) versus SDM coated beads ( in black).

Figure S10. MTDSC thermograms of SDM:4ASA cocrystal coated beads (A) and SDM-PVP coated beads (B). The glass transition can be observed in the reversing heat flow signal (blue line).

Figure S11. Effect of the type of binder on water content and surface area during spray coating.

Figure S12. Effect of the type of binder on the SDM release.

Figure S13. Effect of the bead size on water content and surface area during spray coating.

Figure S14. Effect of the bead size on the SDM release.

Figure S15.  DVS sorption and desorption profile of: a) uncoated (blank) sugar beads 500 µm; b) 5g-Batch of sugar beads 500 µm coated with 95% cocrystal:5% PVP and c) 25g-Batch of sugar beads 500 µm coated with 95% cocrystal:5% PVP.

Figure S16. PXRD patterns of SDM:4ASA physical mixture at different times during the accelerated stability studies.

Figure S17. PXRD patterns of SDM:4ASA polymorph I at different times during the accelerated stability studies.

Figure S18. PXRD patterns of SDM:4ASA polymorph II generated by spray-drying at different times during the accelerated stability studies.