List of Tables:

A Comparative Study between Hot-Melt Extrusion and Spray-Drying for the Manufacture of Anti-Hypertension Compatible Monolithic Fixed-Dose Combination Products

J. F. Kelleher 1 , G. C. Gilvary 2, A. M. Madi 1, D. S. Jones 2, S. Li 2, Y. Tian 2, A. Almajaan 2, Z. Senta-Loys 2, G. P. Andrews2, A. M. Healy 1, *

# Affiliation

1 School of Pharmacy and Pharmaceutical Sciences, Trinity College Dublin, Dublin, Ireland

# 2 School of Pharmacy, Queen’s University of Belfast, Belfast, Northern Ireland

*To whom correspondence should be addressed to:

Anne Marie Healy

Tel: +35318961444

Email: healyam@tcd.ie

Table 1. Details of HPLC gradient elution method including time (min), mobile phase composition and flow rate (ml/min) (%)

| Time (min) | Mobile Phase A (%) | Mobile Phase B (%) | Flow (ml/min) |
| --- | --- | --- | --- |
| 0 | 70 | 30 | 0.8 |
| 5 | 40 | 60 | 1.5 |
| 6 | 70 | 30 | 1 |
| 9 | 70 | 30 | 1 |
| 10 | 70 | 30 | 0.8 |

Table 2. The composition of APIs and excipients in each of the formulations based on a % w/w

|  | HCTZ | RAM | Kollidon VA 64 | PEG 3350 | Soluplus |
| --- | --- | --- | --- | --- | --- |
| Formulation 1 (F1) | 12.5% | 5% | 82.5% | 0% | 0% |
| Formulation 2 (F2) | 12.5% | 5% | 74.25% | 8.25% | 0% |
| Formulation 3 (F3) | 12.5% | 5% | 0% | 0% | 82.5% |

Table 3. Processing conditions used during hot melt extrusion of pharmaceutical formulations.

| Formulation | Feed rate (rpm) | Screw speed (rpm) | Feed Zone (°C) | Zone 1 (°C) | Zone 2 (°C) | Zone 3 (°C) | Die (°C) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| F1 | 10 | 20 | 90 | 110 | 140 | 140 | 120 |
| F2 | 10 | 20 | 70 | 90 | 110 | 110 | 90 |
| F3 | 10 | 20 | 90 | 110 | 140 | 140 | 120 |

Table 4. Overview of particle size analysis (PSA) results of API raw materials and processed formulations

| Sample | Particle Size (µm) (d50) |
| --- | --- |
| HCTZ (Raw) | 28.48 ± 0.13 |
| RAM (Raw) | 8.79 ± 0.22 |
| HME-F1 | 50.48 ± 2.45 |
| HME-F2 | 49.16 ± 4.00 |
| HME-F3 | 36.16 ± 0.74 |
| SD-F1 | 3.41 ± 0.11 |
| SD-F2 | 3.00 ± 0.02 |
| SD-F3 | 3.98 ± 0.01 |

Table 5. Summary of drug content for processed formulations and intrinsic drug dissolution rates from compressed discs in 0.1 M HCl pH 1.2 @ 37 ºC over 120 minutes

| Formulation | HCTZ content (%) | HCTZ dissolution rate (mg/ min/ cm2) | RAM content (%) | RAM dissolution rate (mg/ min/ cm2) |
| --- | --- | --- | --- | --- |
| HME-F1 | 101.44 ± 1.45 | 0.240 ± 0.03 | 90.71 ± 0.65 | 0.087 ± 0.01 |
| HME-F2 | 101.88 ± 2.10 | 0.384 ± 0.04 | 96. 07 ± 0.01 | 0.136 ± 0.02 |
| HME-F3 | 99.64 ± 0.46 | N/A | 85.93 ± 0.33 | N/A |
| SD-F1 | 100.69 ± 0.57 | 0.165 ± 0.02 | 99.54 ± 0.20 | 0.072 ± 0.01 |
| SD-F2 | 100.33 ± 0.74 | 0.239 ± 0.04 | 101.89 ± 1.25 | 0.110 ± 0.01 |
| SD-F3 | 101.25 ± 1.64 | N/A | 100.08 ± 0.26 | N/A |

Table 6. Roughness average (Ra) of the surface of compressed discs for intrinsic dissolution

| Formulation | Roughness average (Ra) (nm) |
| --- | --- |
| SD F1 | 121897 ± 4857 |
| SD F2 | 171079 ± 8641 |
| SD F3 | 148757 ± 24077 |
| HME F1 | 171314 ± 5350 |
| HME F2 | 215656 ± 3188 |
| HME F3 | 174651 ± 7573 |